## Slide 1: Rock dynamics and time dependency
Younus Ahmed Khan

## Slide 2: Strain rate
Rock behaviour mechanisms can occur at significantly different rates:
During the excavation of rock using explosives, rock failure occurs in milliseconds;
A rock block can slip out of a cavern roof in a second;
A shaft might take a day to fill up with water;
A chalk or mudstone face can deteriorate in a few days.
It may take months or years for water to move through a granitic rock mass and,
During the 120 years design life of an unlined rock cavern for civil engineering purposes, creep processes could lead to roof collapse.
Some geological processes occur over millions of years.

## Slide 3: Strain rate
In view of this time dependency over a wide time range, it is convenient to consider the rate at which such processes occur in terms of strain rate
Consider a rock cylinder subjected to uniaxial compression along its axis and that the rock's compressive strength is reached at 0.5% strain, i.e. 0.005 or 5 x l 0 -3 strain. At a strain rate of 1 x l 0 -3 s - 1 , the rock specimen will fail in 5 s.
At a strain rate of 1 x 10 -4 s -1, the rock specimen will fail in 50 s. For explosive failure in 2 ms, the strain rate would be 5 x l0 -3/2 x 10 -3 = 2.5 or 2.5 x 10 ° s -1.

## Slide 4: Stress waves in elastic rocks
For the high strain rates, we can discuss the velocities of propagation of stress waves in elastic rocks, which can be determined as a consequence of Hooke's Law and the equations of motion.
The sum of the rates of changes of the stress components in a given direction is zero when no force is applied, e.g.

## Slide 5
When the sum of these rates of change is not zero (meaning that a net force is applied), then
force = mass x acceleration
or
This is for equilibrium in the x-direction, where p (rho) is the rock density and u is displacement in the x-direction.

## Slide 7
The transverse stress wave, which has a different velocity from the
longitudinal stress wave, can also be referred to as a distortional, shear,
or secondary wave. There are also longitudinal surface (or Rayleigh)
waves, transverse surface (or Love) waves, and Stoneley waves which
occur at the boundary of two connected elastic rock strata.
There is a variety of time-dependent effects at lower strain rates.
Creep occurs when the stress is held constant and the strain changes.
Relaxation occurs when the strain is held constant and the stress changes.
Fatigue occurs when there is increasing strain during stress cycling.

## Slide 8
When the complete stress-strain curve is obtained in uniaxial compression at strain rates of, for example, 1 x 10-3 s - 1 , 1 x 10 -4 s - 1 , and 1 x 10 -5 s -1, the results will be strain rate-dependent: the compressive strength might be 20% higher at a strain rate of 1 x l 0 -3 s-1compared to the compressive strength obtained at a strain rate of 1 x 10 -5 s-l; and the shape of the post-peak curve will be influenced by time-dependent processes.

## Slide 9: Strain Energy, Rock deformation
Definition
Release principles
Energy density

## Slide 10
When an elastic body is deformed-
-the forces (body or surface) that cause the deformation do work on the body as they deform it.
In accordance with the principle of conservation of energy, this work is stored in the deformed body in the form of elastic strain energy.
Elastic strain energy plays an important role in rock mechanics. Physically, strain energy is important because it can potentially cause adverse phenomena such as rock bursts, borehole collapses, etc. (Cook et al., 1966; Salamon, 1984).

## Slide 11
Consider first a cube of rock, of length a on each side-
-that is subjected to a uniaxial stress σ1 in one direction.
Imagine that this stress is applied slowly, so that it increases from 0 to σ1 in a quasi-static manner. This can be represented mathematically by taking the stress to be kσ1, where k is a scalar parameter that increases from 0 to 1.
If the rock is linearly elastic, the strain will increase at a rate proportional to the stress, from 0 to kε1. The stress acts over a face of area a2, so its associated force is kσ1a2.
The final displacement of this face in the direction of the applied stress will be aε1, so that at any intermediate time during the deformation, the displacement is akε1. The incremental work done by this force as the parameter k increases from k to k + dk is therefore given by,
The total work done the force through the entire process of deformation is,

## Slide 12
This work is now stored in the body as elastic strain energy, , so that ETOT =σ1ε1a3/2.
The elastic strain energy per unit volume of rock, which will be referred to as-
-the elastic strain energy density, is = ETOT/a3 = σ1ε1/2
The elastic strain energy stored in this cube of rock, per unit volume, will be given by,
In general,
The principal directions of stress and strain are equal for isotropic case, which is not necessarily the case for anisotropic rocks.

## Slide 13
For isotropic rocks, the stored strain energy density can be written in many
different forms:
1. In terms of normal and shear stresses,
2. In terms of principal stresses,

## Slide 14
3. E can be defined with strains,
4. Again, using principal strains,

## Slide 15
In this stage, the elastic strain energy can be split into two parts:
i) a term that depends on the volume change,
ii) a term that depends on the deviatoric stresses (or strains),
This term is known as the distortional strain energy. It follows that
in order for the strain energy to be positive, the bulk modulus K must satisfy K > 0
if the stress is purely deviatoric, positive-definiteness of the strain energy implies that G > 0.

## Slide 16
5. Can be defined with deviatoric stress and deviatoric strains as well,
where {s1, s2, s3} are the principal deviatoric stresses, {e1, e2, e3} are the principal deviatoric strains, τm is the mean normal stress, and εm is the mean normal strain (which equals one-third of the volumetric strain, εv)

## Slide 17
The assumption is often made that the elastic strain energy should be zero if all
of the strain components are zero, but should be positive whenever at least one
strain component is nonzero.
The total elastic strain energy stored in a body can be found by integrating the elastic strain energy density over the entire body: